| SPECIFICATION TEXT |
| --- |
| PRODUCT | Hydroflam | DATE | 11/06/2015 |
| CE CLASS | P5 | EN STANDARD | EN 312 |

DESCRIPTION

Fire retardant, moisture-repellent and vapour permeable structural construction board with high air-tightness

Hydroflam is a construction board belonging to product class P5 (standard reference EN 312): panels for load-bearing applications for use in humid conditions and in hazard classes of biological attack 1 and 2 of EN 335-3. These panels are therefore in the same area of application as OSB/3 (EN 300), multiplex (EN 636-2).

Hydroflam has fire retardant properties (Euro class B-s2, d0). The panels are self-extinguishing and do not continue to burn once the heat source has been removed. Hydroflam also retains its mechanical strength for a long time in a fire situation. This makes the construction board suitable for use as structural panel in applications where low reaction to fire and limited flame spread are important, and where higher fire-resistance is required.

Hydroflam is an MUF-bonded chipboard with a TopFinish surface. This TopFinish surface provides very high air-tightness (< 0.0025 m³/ m²/h/Pa at 50 Pa; 15 mm). It is important always to seal all joints and gaps with suitable air-tight tape. The composition of construction board limits linear expansion and swelling to a minimum in high air humidity conditions.

In timber-frame constructions and low-energy and passive house buildings, Hydroflam can be used as a reinforcing exterior wall, as part of a façade or as a partition wall. When used as a façade element, Hydroflam must be protected with a rain screen.

STANDARD DIMENSIONS

Standard dimension: 2,800 x 1,196 x 12 mm (H x W x D)

Various thicknesses and lengths/widths for compressing and finishing can be discussed. Contact our agent about this or send an email to info.panels@unilin.com.

TECHNICAL SPECIFICATIONS

|  | Reference | Value |
| --- | --- | --- |
| Declaration of performance (DOP) | DOPDurelisStormBlockv1 |
| Product type |  | Fire-retardent reinforcing construction board |
| CE class |  | P5 |
| Reference standard | EN 312 | Wood-based panel material |
| AVCP class: |  | 1 |
| Certificate number |  | 1161-CPR-1323 |
|  | Thickness class (mm) |
| Panel material | EN13986 | 10 | 12 | 13 | 16 | 18 | 19 | 22 |
| Density (kg/m³) | EN323 | NPD | 780 | NPD | 750 | 750 | 740 | 740 |
| Bending strength (N/mm²) | EN312, table 7 | 18 | 18 | 18 | 16 | 16 | 16 | 14 |
| Bending stiffness (N/mm²) | EN312, table 7 | 2550 | 2550 | 2550 | 2400 | 2400 | 2400 | 2150 |
| internal bond (N/mm²) | EN312, table 7 | 0.45 | 0.45 | 0.45 | 0.45 | 0.45 | 0.45 | 0.40 |
| Swelling after 24h (%) | EN312, table 7 | 13 | 11 | 11 | 10 | 10 | 10 | 10 |
| Moisture resistance option 1: internal bond (N/mm²) | EN312, table 8 | 0.25 | 0.25 | 0.25 | 0.22 | 0.22 | 0.22 | 0.20 |
| Moisture resistance option 1: thickness swelling (%) | EN312, table 8 | 12 | 12 | 12 | 12 | 12 | 12 | 11 |
| Formaldehyde class | EN13986, table B1 | E1 | E1 | E1 | E1 | E1 | E1 | E1 |
| Formaldehyde content (mg/100g) | EN120 | ≤ 2 | ≤ 2 | ≤ 2 | ≤ 8 | ≤ 8 | ≤ 8 | ≤ 8 |
| Reaction to fire | EN13501-1 | B-s2,d0 | B-s2,d0 | B-s2,d0 | B-s2,d0 | B-s2,d0 | B-s2,d0 | B-s2,d0 |
| Water vapour permeability µ (wet) | EN12986, table 9 | 16 | 16 | 16 | 16 | 16 | 16 | 16 |
| Water vapour permeability µ (dry) | EN12986, table 9 | 50 | 50 | 50 | 50 | 50 | 50 | 50 |
| Moisture content (%) | EN322 | 6-10 | 6-10 | 6-10 | 6-10 | 6-10 | 6-10 | 6-10 |
| Airborne sound insulation (dB) | EN13986, chp 5.10 | NPD | NPD | NPD | NPD | NPD | NPD | NPD |
| Sound absorption (α) | EN13986, table 10 | 0.10/0.25 | 0.10/0.25 | 0.10/0.25 | 0.10/0.25 | 0.10/0.25 | 0.10/0.25 | 0.10/0.25 |
| Thermal conductivity λ (W/m.K) | EN13986, table 11 | 0.14 | 0.14 | 0.14 | 0.14 | 0.14 | 0.14 | 0.13 |
| Strength - tension ft (N/mm²) | EN12369-1 | 9.4 | 9.4 | 9.4 | 8.5 | 8.5 | 8.5 | 7.4 |
| Strength - compression fc (N/mm²) | EN12369-1 | 12.7 | 12.7 | 12.7 | 11.8 | 11.8 | 11.8 | 10.3 |
| Strength - bending fm (N/mm²) | EN12369-1 | 15.0 | 15.0 | 15.0 | 13.3 | 13.3 | 13.3 | 11.7 |
| Strength - panel shear fy (N/mm²) | EN12369-1 | 7.0 | 7.0 | 7.0 | 6.5 | 6.5 | 6.5 | 5.9 |
| Strength - planar shear fr (N/mm²) | EN12369-1 | 1.9 | 1.9 | 1.9 | 1.7 | 1.7 | 1.7 | 1.5 |
| Stiffness - tension Et (N/mm²) | EN12369-1 | 2000 | 2000 | 2000 | 1900 | 1900 | 1900 | 1800 |
| Stiffness - compression Ec (N/mm²) | EN12369-1 | 2000 | 2000 | 2000 | 1900 | 1900 | 1900 | 1800 |
| Stiffness - bending Em (N/mm²) | EN12369-1 | 3500 | 3500 | 3500 | 3300 | 3300 | 3300 | 3000 |
| Stiffness - panel shear Gv (N/mm²) | EN12369-1 | 960 | 960 | 960 | 930 | 930 | 930 | 860 |
| Impact resistance (class) | EN12871 | NPD | NPD | NPD | NPD | NPD | NPD | NPD |
| Linear expansion δI30.85 (mm/m) | EN318 | < 3 | < 3 | < 3 | < 3 | < 3 | < 3 | < 3 |
| Mechanical durability (kmod;kdef) |  | EN1995-1-1 | EN1995-1-1 | EN1995-1-1 | EN1995-1-1 | EN1995-1-1 | EN1995-1-1 | EN1995-1-1 |
| Biological durability (class) | EN335 | Class 1 & 2 | Class 1 & 2 | Class 1 & 2 | Class 1 & 2 | Class 1 & 2 | Class 1 & 2 | Class 1 & 2 |
| Pentachlorophenol (PCP) content (ppm) | EN13986, chp 5.18 | < 5 | < 5 | < 5 | < 5 | < 5 | < 5 | < 5 |